Date: Tue, 27 Nov 2001 16:08:31 -0800

From: Lynne Fieber <lfieber@rsmas.miami.edu>

Chloriding Solution

250 ml HCl (37%)

50 ml H20

25 g FeCl3

This is a lifetime supply. Store in foil wrapped glass container of ample volume. Expect the foil covering the top to corrode away now and then. Handle with care. Dip electrode into this solution (I pour some into a small weigh boat, then immerse my electrode, but you will come up with your own solution) until desired darkness (10' or less), then rinse well with deionized water. Repeat as necessary, once per week for pipette holder getting heavy use.

The first time you coat new silver wire you will probably need to rough up the surface very gently with some really fine sandpaper or XXX steel wool to get the chloriding solution to stick.