DHT Implant Protocol

Needle Prep:

20-gauge needle

Dremel tool

Cut-off Wheel

Eye protection

1 ml syringe

- Attach cut-off wheel to Dremel tool using the correct size collet and tighten the collar as much as possible before cutting.

- Using the cut-off wheel, cut off tip of 20-gauge needle to leave a stub of approximately 3 mm

- Sand rough edges with cut-off wheel so the needle is short, but smooth (be careful not to melt the bore closed while sanding)

- Tightly attach needle to 1 ml syringe

Implant Prep: Instructions are for a 2:3 DHT: Silicone Mix

Silicone

Weigh paper

DHT

Spatula

CAUTION:  Use precautionary measures when handling DHT.  Take the cap off under the hood, wear gloves (females especially), be extremely careful not to spread any around the lab and clean all surfaces and equipment thoroughly after use.

- Wipe down all surfaces you will be using so that you can see any DHT that may have gotten away from you

- Tare a sheet of weigh paper

- Squeeze a dab of silicone onto weigh paper and measure out 300 mg

- Clean spatula and tare a new sheet of weigh paper

- Measure out 200 mg of DHT

- Carefully place the DHT onto the paper with silicone and gently mix into a consistent paste

- Make sure needle is tightly fitted to syringe, remove plunger, and carefully load the paste into the syringe

- Clean the spatula with ethanol and Kim wipes after contact with DHT paste – (rinse with ethanol, wipe off with Kim wipes, rinse with ethanol and wipe with Kim wipes, rinse with RO water)

Implant Prep:

Weigh paper

DHT paste

Sharpie

Syringe & Needle

- Label weigh paper with implant composition, ratio, and date it was created

- Squeeze paste onto weigh paper in long, straight strips

(TIP:  It seems to be easiest to keep the needle still and move the paper away from the needle to create straight lines)

- Dry implants under the hood for 24 hours

- Place implants in petri dishes to cure for 2-3 days before use

- Clean work space thoroughly!